## Slide 1
0
Cell capacity (mAh)
qp mp
qn mn
p
n
Inventory
Inventory = qpmp – abs(p - n) Abs = absolute value
0
Cell capacity (mAh)
qp mp
qn mn
p
n
Inventory
Anode limited
cathode limited
Inventory = qpmp – abs(p) Abs = absolute value
This is for the first cycle that you analyse

## Slide 2
0
Cell capacity (mAh)
qn mn
p
n
Inventory
Inventory = qpmp – abs(p - n) Abs = absolute value
Anode limited
This is after a bunch of cycles
For the anode limited cell, the SHIFT LOSS, due to thickening of the anode SEI is NOT QUITE equal to the Inventory Loss. This is because the upper cutoff of the positive VERSUS lithium (and hence qp) changes slightly as the graphite curve shifts to the right.
The SHIFT LOSS is abs[ (p - n)cycle n - (p - n)first cycle]

## Slide 3
0
Cell capacity (mAh)
qp mp
qn mn
p
n
Inventory
Initially cathode limited
Inventory = qpmp – abs(p) Abs = absolute value
For the initially cathode limited cell the SHIFt Loss is AGAIN
SHIFT LOSS = abs[(p - n)cycle n - (p - n)first cycle]